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MAXXOL MXO T-Hydraulic HLP 32 is a range of mineral based hydraulic oils containing rust and corrosion inhibitors and also an anti-wear additive to ensure protection of equipment and pumps operating under severe service and high pressure conditions. They are recommended for use in industrial and mobile applications, operating under mild or severe conditions. Also excellent products for general industrial equipment, including machine tools, rotary air compressors, torque converters and enclosed gearboxes.

Features
• Excellent Hydrolytic Stability
• Outstanding thermal and oxidative stability
• Superior rust protection
• Minimal increases in air entrainment
• Very good demulsibility performance

	Performance Level

	Denison HF-0, HF-1, HF-2 (2005),  DIN 51524 part I, II (2004),
Cincinnati Lamb P-68, P-69 and P-70,  Eaton I-286-S3,
ASTM D6158,  FZG A/8.3/90 load stage 10 pass,
Excellent wear protection in the Vickers 104C vane pump test



	Typical Properties
	
	
	ISO VG 32
	

	Specific Gravity (15/4℃)
	
	
	0.8659
	

	Kinematic Viscosity (100℃, cSt)
	
	
	5.485
	

	Kinematic Viscosity (40℃, cSt)
	
	
	32.35
	

	Viscosity Index 
	
	
	105
	

	Flash Point (℃)
	
	
	212
	

	Pour Point (℃)
	
	
	-35.0
	

	Copper Strip Corrosion
	
	
	1a
	



· Values shown are typical and may vary
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