Integrating lubricant technologies

PRODUCT INFORMATION

MAXXOL MXX HYDRO LUBE AW 46

MAXXOL MXX HYDRO LUBE AW 46 range of hydraulic oils based on highly purified mineral oil enriched with a system of stabilizing zinc additives. Used in hydraulic systems that require wear protection, such as pulleys, variable speed devices and bearings

Features

- High oxidation stability

- High moisture separation and air insulation

- Good corrosion and abrasion resistance

Performance Level

VG 46

| Typical Properties |  |  | ISO VG 46 |  |
| --- | --- | --- | --- | --- |
| Specific Gravity (15/4℃) |  |  | 0.8544 |  |
| Kinematic Viscosity (40℃, cSt) |  |  | 43.8 |  |
| Viscosity Index |  |  | 167 |  |
| Flash Point (℃) |  |  | 232 |  |
| Pour Point (℃) |  |  | -36 |  |

- Values shown are typical and may vary