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PRODUCT INFORMATION

MAXXOL MXX HYDRO LUBE AW 46

MAXXOL MXX HYDRO LUBE AW 46 range of hydraulic oils based on highly purified mineral oil enriched with a system of stabilizing zinc additives. Used in hydraulic systems that require wear protection, such as pulleys, variable speed devices and bearings
Features
- High oxidation stability
- High moisture separation and air insulation
- Good corrosion and abrasion resistance

	Performance Level

	VG 46



	Typical Properties
	
	
	ISO VG 46
	

	Specific Gravity (15/4℃)
	
	
	0.8544
	

	Kinematic Viscosity (40℃, cSt)
	
	
	43.8 
	

	Viscosity Index 
	
	
	167
	

	Flash Point (℃)
	
	
	232
	

	Pour Point (℃)
	
	
	-36
	

	
	
	
	
	



· Values shown are typical and may vary
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