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TURBO CX 7 5W30
Turbo CX 7 is specially formulated for the lubrication needs of modern gasoline and diesel cars and RV/SUV with DPF. Formulated with advanced base stocks, premium additives. Turbo CX 7 contains high quality anti-wear additives and surpasses the tough ACEA oil specifications for high temperature/high shear viscosity. It provides outstanding protection in high RPM, hot running engines.Turbo CX 7 is recommended specially for diesel engines with the after-treatment system which fulfill the EURO IV. Turbo CX 7 holds the effectiveness of the after-treatment system for very long term.
Advantage : 

· Reduced evaporation tendency 
· Very good cold start properties

· Very good protection against sludge

· Reduced wear of cylinder and camshaft

· Reduced fuel consumption thanks to smooth running properties 

	Performance Level
	
	Viscosity Grade

	API SP/ ACEA C2
	
	SAE 5W30


	Typical Properties
	
	SAE 5W30

	Specific Gravity (15/4℃)
	
	0.8526

	Kinematic Viscosity (100℃, cSt)
	
	11.4

	Kinematic Viscosity (40℃, cSt)
	
	67.57

	Viscosity Index 
	
	163

	Flash Point (℃)
	
	234

	Pour Point (℃)
	
	-33

	CCS Viscosity (cP)
	
	6,021 (-30℃)

	TBN (mg·KOH/g)
	
	7.94

	TAN (mg·KOH/g)
	
	1.78


· Values shown are typical and may vary
